Spectrum processing :

Peak possibly omitted : 3.311 keV

Processing option : All elements analyzed (Normalised)

Number of iterations = 2

Standard :

O    SiO2   1-Jun-1999 12:00 AM

Mn    Mn   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% |  |
| --- | --- | --- | --- |
| O K | 49.74 | 77.27 |  |
| Mn K | 50.26 | 22.73 |  |
| Totals | 100.00 |  |  |

Comment:

1/13/2026 10:30:32 AM

Project 1